## Slide 1
Jennifer A. Clark
Jack F. Douglas
Hydration Contribution to the Solvation Free Energy of Water-Soluble Polymers DOI: 10.1021/acs.jpcb.5c01009

## Slide 2: Thermodynamics of Dynamic Hydration Layer

## Slide 3: Temperature Response of Polymers
We can likely apply learnings from the protein literature to understand polymer phase behavior
Riccio & Graziano, Chemical Physics Letters, 794 (2022)
Proteins: Hot and Cold Denaturization
Polymers: LCST and UCST
Tenhu and Niskanen DOI:10.1039/C6PY01612J

## Slide 4: Salt Response of Polymers
Proteins
Anti-Polyelectrolyte Effect
Polymers
Increase in salt concentration increases chain dimensions
Salt type combination alters the effect
[NaCl]
Delgado & Schlenoff. Macromolecules, 50 (2017)
Polyelectrolyte Effect

## Slide 5
Zwitterionic Polymers: Therapeutic Excipient
However, some polybetaines can interact with and lower the barrier of denaturization for some proteins
“Zwitterionic polymers are gaining attention as alternatives to PEG [as a therapeutic excipient] for their ability to stabilize proteins against denaturation and evade immune recognition while maintaining extended circulation in vivo”
- Pharmaceutics (2023)
Fundamental understanding of the polybetaine solution behavior is needed for therapeutic solution design
Under Investigation at NIST
Kisley et al. Biomacromolecules, 19 (2018)
Pickett et al. J. Chem. Phys., 159 (2023)
Notes: Of course neutral soluble polymers are still used in formulation applications for paint and coatings, often with trial and error.

## Slide 6: Extended Hydration From THz Spectroscopy
Ebbinghaus, et al. Proc. Natl. Acad. Sci. 2007, DOI: 10.1073/pnas.0709207104.
Nibali and Havenith JACS 2014 DOI: 10.1021/ja504441h
Spectroscopic studies reveal a hydration region extending from 10 Å to more than 18 Å.1 (3 to 6 water diameters)
It is appreciated that the hydration layer can actively facilitate protein binding and folding.2
Vibrational density of states (VDOS) indicates that only the THz frequencies discern between degrees of bound water
Pattni et al. JPC B, 2017, DOI: 10.1021/acs.jpcb.7b03966
Notes: Edwin J. Heilweil – 683.12 Nanoscale Spectroscopy Group
David F. Plusquellic – 686.11 Molecular and Bio-Photonics Group
Also, Dr. Andrea Markelz at UB uses terahertz spectroscopy to study proteins.

## Slide 7: Debye-Waller Parameter: Context
The MSD after 1ps, , reveals a gradient in the water interfacial mobility[2]
Amyloid-β Fibril Hydration
Haddadian et. al. J. Chem. Phys 154 (2021)
VDOS is a computationally expensive calculation, Is there a cheaper alternative?
Our development is based on these observations
From the “shoving” model, relaxation events where a particle escapes from its local cage…
…should be approximately equal to the shear elastic energy cost for this displacement.
Others have then linked to short-time molecular displacements.
where is the Debye-Waller parameter, defined as the MSD on the caging timescale (~1 ps).
Notes: Elastic models of glass-forming liquids assume that relaxation events are triggered by thermal fluctuations creating a sufficient expansion of a local volume, leading to the conjecture that the relaxation time is related to the high-frequency shear modulus, which, in turn, is linked to short-time molecular displacements
for a range of T and for a range of models of the potential for water. The result is evidently general and remarkable

## Slide 8: Hydration Comparison
Higher temperature and introduction of salt decrease relative (i.e., Debye-Waller parameter) indicating a stiffer chain
We have quantified and visualized the dynamic hydration layer for these polymers
Clark, Prabhu, Douglas . JPC B 127, 38, 8185 (2023) DOI: 10.1021/acs.jpcb.3c03654
8

## Slide 9: Ion Effects on Linear Polymer Solvation
For a single linear chain in this constrained configuration, we regain the intended value of with a constant entropic contribution (in theory)
taken from Andreev et al.
to avoid convolution of preferred ion interactions
{
0.4, # Hydrophobic
1.0, # Neutral
2.0 # Hydrophilic
}
Entropy of Polymer
0
=1
=1
{ 0.4, 1.0, 2.0}
Entropy of Solvent
Enthalpy of Solvent
Notes: Discuss Flory and Krigbaum39
FH theory does not address hydration interactions between polymers and the solvent that can lead to large entropic effects to the free energy of mixing.
describe solvation by treating the polymer-solvent interaction as a reversible binding equilibrium between the solvent and polymer and controlled by enthalpic and entropic thermodynamic energetic parameters.

## Slide 10: Radial Distribution Function: T* = 0.7
↑ values ↑ Structure
rBackbone

## Slide 11: Dynamic Hydration Layer: T* = 0.7
↑ values ↑ Structure
↑ values ↓ <u2>
For atomistic work, <u2>/<> ranged from ~0.3 to unity
rBackbone

## Slide 12: Dynamic Hydration Layer
1 mol/L salt solutions
<u2> consistent with Chaotropic / Kosmotropic Ion Trends for all values
No r dependence!
= 0.85
Influence of the polymer extends to 3 , that’s an influence on 20x the volume that it occupies
has a larger local effect than salt
= 0.4
= 2.0
= 1.25
Can we see this effect in ?
rBackbone

## Slide 13: Free Energy Contributions of Solvation
0.54 ± 0.01) = 0
0.883 ± 0.005) = 0
0.54 ± 0.01) = 0
This shows entropic contribution from dynamic hydration!
Unexpected temperature
dependent change in
Enthalpy
Temperature dependence switches with hydrophilicity

## Slide 14: Coordination
Fairly constant coordination in the bulk: 12
=
Only at high , 12
11
10
What happens in the dynamic hydration layer?
RDF Min (1.57 ± 0.01)
RDF Min: (1.51 ± 0.01)

## Slide 15: Coordination with in 2.5 from Polymer
In the bulk: ranges from 12.1 to 12.4
=
Only at high , 12
11
10
Solution beads in the dynamic hydration layer exhibit reduced coordination, especially at high T* and low
RDF Min (1.57 ± 0.01)
RDF Min: (1.51 ± 0.01) (1.53 ± 0.03)

## Slide 16: Kirkwood Buff Integrals
Krikwood Buff Theory provides a metric:
Represents the excess (or deficiency) in the average number of molecules, i, around molecule j
These quantities convey information on the average "affinity" between these molecules
Ben-Naim developed an inversion procedure for Kirkwood Buff Theory to calculate from experimental data such as:
partial molar volumes
isothermal compressibilities
partial vapor pressures
In simulations we can calculate these directly for experimental comparison, or in our case assessing co-solvent interactions with the polymer
Ben Naim J. Chem. Phys. 67, 4884–4890 (1977) DOI: 10.1063/1.434669

## Slide 17: Kirkwood Buff Integral: Polymer-Solvent

## Slide 18: Ion Partitioning
rBackbone
Notes: Likely less NaCl because of hydration layer
Increase in CsCl is interesting and reminiscent of tendency for Cs to be drawn toward interfaces

## Slide 19: Where are we now?
We’ve isolated the thermodynamic effects of polymer solvation and found
greatly outweighs for interactions on the order of charged polymers
For low polymers, ↑T ⇒ ↓
  i.e., LCST
For high polymers, ↑T ⇒ ↑
  i.e., UCST
Specific ion effects:
  do not appear in the free energy changes (for this toy system where )
  do appear in partitioning and Kirkwood Buff Integrals
Kirkwood Buff Integrals illustrate changes in solvent-solvent affinity in the dynamic hydration layer
Coordination number of the polymer and the solvent change with
Small changes in with respect to T seem to correlate with changes in coordination number

## Slide 20
Thank You
NRC Research Associateship Programs
Project Members:
Jack F. Douglas
Vivek M. Prabhu
Debbie Audus
Robert Ivancic
Jeremy Wang
Funding:
Contact Information:
Email: jennifer.a.clark13@gmail.com
Acknowledgments:
Mauro Mugnai
Iván Pulido
Michael Shirts